## Slide 1: SiC MOSFETs: Gate Drive Optimization
Steve Mappus

## Slide 2: Agenda
SiC Introduction
SiC MOSFET characteristics
SiC MOSFET dynamic switching
Discrete SiC gate drive circuit
NCP51705 SiC MOSFET gate driver
  Distinguishing features
  System performance
  Application circuit (EVB)
NCP51705 parametric test results
  Double pulse test
Closing Summary

## Slide 3: SiC Introduction

## Slide 4: Si Verses WBG Material Properties
Properties | Si | 4H-SiC | GaN
Bandgap Energy (eV) | 1.12 | 3.26 | 3.50
Electron Mobility (cm2/Vs) | 1400 | 900 | 1250
Hole Mobility (cm2/Vs) | 600 | 100 | 200
Breakdown Field (MV/cm) | 0.3 | 2.0 | 3.5
Thermal Conductivity (W/cm°C) | 1.5 | 4.9 | 1.3
Maximum Junction Temperature (°C) | 150 | 600 | 400
Think SiC: High voltage, high frequency, very high temperature!

## Slide 5: SiC MOSFET Characteristics
Most Critical for Gate Drive

## Slide 6: SiC MOSFET: ID vs VDS Output Characteristics
SiC has no linear/saturation distinction
Behaves like voltage controlled resistor
Need over current protection (“DESAT”)
Modest transconductance = low gain:
Require large VGS to force large ID:
Consider two ID vs VDS operating points, “A” and “B”:
RDS is 2.3 times higher for VGS=12 V
SiC MOSFETs operate best at VGS=20 V

## Slide 7: SiC MOSFET: On Resistance
PTC: Increase TJ=Increase RDS
NTC: Increase TJ=Decrease RDS
For Si MOSFET whenever VGS>VTH, RDS has PTC
SiC has NTC for VGS<16 V
  ΔRDS/ΔTJ slope is negative
  Can not be easily paralleled for VGS<16 V
RDS≈RCH+RDRIFT+RJ
  RDRIFT+RJ are PTC resistances
    Dominant at high VGS
  RCH is NTC resistance
    Dominant at low VGS
Gate driver should be rated for VDD ≥ 25 V

## Slide 8: SiC MOSFET: Internal Gate Resistance, RGI
Relatively high RGI
Much lower CISS
Slightly lower CGD & COSS
RGI is inversely proportional to die size
Smaller SiC die means higher RGI
But….
  Lower QG
  Lower Ciss
  Lower RGIxCiss time constant
 | SiC_1 | SiC_2 | Si_1 SJ FET | Si_2 SJ FET
BVDSS (V) | 1200 | 1200 | 900 | 650
ID (A) | 19 | 22 | 36 | 15
RDS (mΩ) | 160 | 160 | 120 | 130
QG (nC) | 34 | 62 | 270 | 35
QGD (nC) | 14 | 20 | 115 | 11
CISS (pF) | 525 | 1200 | 6800 | 1670
COSS (pF) | 47 | 45 | 330 | 26
VGS (V) | -5 to 20 | -6 to 22 | ±20 | ±20
VGS(TH) (V) | 2.5 | 2.8 | 3 | 3.5
RGI (Ω) | 6.5 | 13.7 | 0.9 | 1
RGIxCISS (ns) | 3.4 | 16.4 | 6.1 | 1.7
Gate driver output impedance should be as low as possible

## Slide 9: SiC MOSFET: Gate Charge
Gate charge loss limits operating frequency
Negative gate drive during off-time
  RGI is high
  VGS<0 V to ensure fast dVDS/dt
  dVDS/dt immunity against low VTH
Miller plateau
  Higher VGS compared to Si
  Not flat due to low gm
Gate driver should be rated for -5 V<VGS(MIN)<-2 V

## Slide 10: SiC MOSFET Dynamic Switching

## Slide 11: SiC MOSFET Switching: Turn-On
t0→t1: VGS<VTH, gate drive delay
t1→t2: VTH<VGS<VGS(MP), ID is increasing
t2→t3: VGS=VGS(MP), VDS discharges
  Need high IG during this interval
t3→t4: VGS>VGS(MP),
  RDS(ON) reaches minimum value and has PTC
Gate driver should be rated for high IG (ISRC) at VGS(MP)

## Slide 12: SiC MOSFET Switching: Turn-Off
t0→t1: VDD<VGS<VTH(MP), RDS(ON) increasing
t1→t2: VGS=VGS(MP), VDS increasing
t2→t3: VGS=VGS(MP), ID decreasing, body-diode blocking
t3→t4: VGS(MP)<VGS<VEE,
  RDS reaches maximum value
  Need high IG (ISNK) during this interval
Gate driver should be rated for high IG (ISNK) at VEE<VGS<VGS(MP)

## Slide 13: SiC MOSFET Gate Driver Requirements
Summary of SiC gate drive requirements
  Able to withstand 35 V rail-to-rail (VDD=25 V and VEE=-10 V)
  VGS must have fast rise and fall edges (~few ns)
  High ISRC across the Miller plateau (several amps)
  Must have high ISNK to guarantee hold off and high dVDS/dt immunity
  VDD UVLO level matched to SiC thermal capabilities
  DESAT function for monitoring over current across SiC MOSFET RDS(ON)
  Low parasitic inductance package
  Small driver package able to be located close to SiC MOSFET

## Slide 14: Discrete SiC Gate Drive Circuit

## Slide 15: SiC “Discrete” Gate Drive Example
General purpose low-side gate driver
  VDD(MAX)>25 V
Requires two dc-dc converters
  Post-regulation for isolator 5-V bias
  Low transformer winding capacitance. Example:
BUT…
  Limited driver choices
  No DESAT protection
  VDD UVLO based on 12 V
  No VEE UVLO

## Slide 16: Integrated SiC Gate Drive Circuit

## Slide 17: NCP51705 SiC Gate Driver
Features
  VDD rated for 28 V
  ISRC=6 A, ISNK=10 A at ~VDD/2
  5 V, 20 mA bias regulator
  Separate signal, power ground
  Separate OUTSRC, OUTSNK
  Internal thermal shutdown
  Separate IN+, IN- TTL inputs
“Differentiating” Features
  DESAT, OCP
  Internal VEE charge pump
  Programmable VDD UVLO
  XEN, fault and driver “status”
  4 mm x 4 mm MLP

## Slide 18: NCP51705 DESAT
DESAT is in addition to PWM OCP
Protects SiC MOSFET against excessive power dissipation
  RDS↑, VDS↑ while ID is maximum
  VDD or VGS too low
  Short-circuit or overload
Monitors VDS only during on-time
  500ns timer allows VDS time to fall
Programmable by R1, D1 selection
Select D1 with lowest CJ

## Slide 19: NCP51705 VEE Charge Pump, VEESET
390 kHz fixed frequency (290 kHz option)
Three small SMD ceramic capacitors
VEE UVLO ~80 % set value
VEE programmable by VEESET
  VEESET=GND, VEE UVLO is disabled
VEESET | COMMENT | VEE | VEE(UVLO)
VDD | 9 V<VEESET<VDD | -8 V | -6.4 V
V5V |  | -5 V | -4 V
OPEN | Add CVEE≤100 pF from VEESET to SGND | -3 V | -2.4 V
GND | Remove CVEE and connect VEE to PGND | 0 V | NA
GND | Connect VEE to external negative voltage rail | -VEXT | NA

## Slide 20: NCP51705 UVSET
Active at VDD=7 V
Fixed 1 V, VDD UVLO hysteresis
  VOFF=VON-1 V
Two UVLO conditions to enable OUT
  VDD>VON
  VEE<80 % set value
  RUVSET chosen for desired VON by:

## Slide 21: NCP51705 UVSET, HV Start-Up Considerations
Set VON=17 V, shallow CVCC discharge ramp:
Set VON=12 V, deep CVCC discharge ramp:
Small CVCC, low VGS start on SiC
Large CVCC, high VGS start on SiC

## Slide 22: NCP51705 Package
4 mm x 4 mm MLP
  Low inductance
  Double pins, double bond for power connections
  digital on left side for easy PWM interface
  Bottom pad is electrically isolated, thermally conductive; heatsink to PCB (do not connect to PGND or SGND)
Power dissipation concerns
  Disable internal charge pump, use external VEE
  No load on V5V (5 V)
  Lower switching frequency
  Get creative with top side heatsinking
SiC MOSFETs mostly stuck in TO-247 packages

## Slide 23: NCP51705 Start Up
VDD_UVLO(ON)=12 V
  VDD=14.94 V, VEE=-4 V (80 % of -5 V)
  VEE UVLO Dominates
VDD_UVLO(ON)=18 V
  VDD=18.45 V (VEESET point), VEE=-5 V
  VDD UVLO Dominates

## Slide 24: NCP51705 VEE Start Up
VEE slow control loop
  Slight undershoot
  ~400 µs correction
  Regulates to -3 V, -5 V or -8 V by VEESET pin strapping
VEESET | COMMENT | VEE | VEE(UVLO)
VDD | 9 V<VEESET<VDD | -8 V | -6.4 V
V5V |  | -5 V | -4 V
OPEN | Add CVEE≤100 pF from VEESET to SGND | -3 V | -2.4 V
GND | Remove CVEE and connect VEE to PGND | 0 V | NA
GND | Connect VEE to external negative voltage rail | -VEXT | NA

## Slide 25: NCP51705 Shut Down
Smooth shutdown, no glitch pulses
  OUT stops switching, tracks VEE discharge
VDD_UVLO(ON)=18 V
  VDD=17 V off (18 V-1 V hysteresis)
  OUT pulse terminates when VDD<17 V

## Slide 26: NCP51705 Propagation Delay
Turn-on, VDD=12 V, COUT=1 nF
  19 ns, 90 % IN+ to 10% OUT
  tRISE≈5 ns
Turn-off, VDD=12 V, COUT=1 nF
  22 ns, 10% IN+ to 90% OUT
  tFALL≈5 ns

## Slide 27: NCP51705 DESAT
Normal operation, 80 kHz, 100 pF
  VDESAT=5 V (<7.5 V threshold)
Fault operation, 30 kHz, 100 pF
  VDESAT=7.5 V
  OUT trailing edge terminated

## Slide 28: NCP51705 Mini EVB
35 mm x 15 mm, TO-247

## Slide 29: NCP51705 Mini EVB
Option 1 (preferred) - Horizontal mounting
Option 2 – Vertical mounting
Mounting into existing power PCB
Hardwire to EVB
  XVDD/XGND (digital isolator primary +5 V)
  VDD/GND (NCP51705 +20 V)
  IN+/XGND (PWM input signal)

## Slide 30: Parametric Test Results

## Slide 31: Double Pulse Test
Clamped inductive switching
Compare switching performance between NCP51705 mini EVB and basic SiC opto-coupler driver

## Slide 32: VGS Dynamic Switching
VGS rising
  1.2 kV SiC MOSFET load
  VDS=600 V, ID=30 A, -5 V<VGS<20 V
VGS falling
  1.2 kV SiC MOSFET load
  VDS=600 V, ID=30 A, -5 V<VGS<20 V

## Slide 33: VDS Dynamic Switching, Vary RGATE
NCP51705 VDS rising
  VDS=600 V, ID=30 A, -5 V<VGS<20 V
  1.1:1 dVDS/dt variation for 1 Ω<RGATE>15 Ω
FOD8384 VDS rising
  VDS=600 V, ID=30 A, -5 V<VGS<20 V
  2.3:1 dVDS/dt variation for 1 Ω<RGATE>15 Ω

## Slide 34: VDS Dynamic Switching
NCP51705 vs FOD8384 compare
  VDS=600 V, ID=30 A, -5 V<VGS<20 V, RGATE=1 Ω
  NCP51705, faster dV/dt, better damping, less ringing
NCP51705 VDS rising, -6 V<VEE<0 V
  VDS=600 V, ID=30 A

## Slide 35: Closing Summary
Gate drive: Most critical but often overlooked
Simple, reliable, high performance gate drive is critical for SiC success
NCP5170
  Simple
  Flexible
  High-speed
  Minimal components
  Reliable